Supplementary Information

An Interpretable Nano-QSAR Framework for Predicting Dermal Cytotoxicity of Gold and Silver Nanoparticles

Qingwei Yua, Peiyao Liua, Huimin Wanga, Zhongjie Huaa, Ying Tanga*

a Beijing Key Laboratory of Plant Resources Research and Development, School of Light Industry Science and Engineering, Beijing Technology and Business University, Beijing 100048, China

*Correspondence: Ying Tang, Beijing Key Laboratory of Plant Resources Research and Development, School of Light Industry Science and Engineering, Beijing Technology and Business University, Beijing 100048, China

Email addresses: Q. Yu (2431041301@st.btbu.edu.cn); P. Liu (2431042194@st.btbu.edu.cn); H. Wang (bnfxdd@163.com); Z. Hua (Y30240492@mail.ecust.edu.cn); Y. Tang (tangying@th.btbu.edu.cn)

Table S1. Numerical codes for categorical variables

| Variable | Code | Reductant | Code | Variable | Code |
| --- | --- | --- | --- | --- | --- |
| Material |  | Undefined (Purchased) | 1 | Extractant |  |
| Au | 0 | Conjugate (Deposition and Precipitation) | 2 | N/A (0) | 1 |
| Ag | 1 | Sodium borohydride | 3 | water | 2 |
| Shape |  | Sodium citrate | 4 | ethanol | 3 |
| sphere | 1 | Hydroxylamine | 5 | glycol | 4 |
| rod | 2 | Ascorbic acid | 6 | water-ethanol | 5 |
| branch | 3 | Hydroxyethyl piperazine ethanesulfonic acid | 7 | water-ethanol-methanol | 6 |
| polyhedron | 4 | Flavonoid | 8 | Synthesis method |  |
| star | 5 | Polysaccharide | 9 | chemical | 1 |
| flower | 6 | Polyvinylpyrrolid one | 10 | biological | 2 |
| mixture | 7 | Polyethylene glycol (PEG) | 11 | physics | 3 |
| Cell_type |  | Surfactant | 12 | Coating |  |
| Immortalized | 0 | Lysozyme protein | 13 | N/A | 1 |
| Primary | 1 | Plant extract | 14 | carboxyl group | 2 |
| Via_test |  | Electrochemical (high_voltage) | 15 | flavonoids | 3 |
| JC-1 | 1 | Cell_line |  | tannic acid | 4 |
| XTT | 2 | hSSCs | 1 | cationic surfactant | 5 |
| LDH | 3 | NCTC | 2 | polysaccharide | 6 |
| Alamar blue | 4 | NHEK | 3 | Polyethylene glycol (PEG) | 7 |
| SRB | 5 | KMST | 4 | protein | 8 |
| MTS | 6 | HSF | 5 | phytochemicals | 9 |
| LIVE/DEAD | 7 | HFF | 6 | polyphenol | 10 |
| NRU | 8 | HaCaT | 7 | sodium citrate | 11 |
| MTT | 9 | HDF | 8 |  |  |

Table S2. Hyperparameter configurations for different machine learning models

| Model | Hyperparameter Setting |
| --- | --- |
| LightGBM | metric=RMSE, n_estimators=250, learning_rate=0.02, max_depth=4, num_leaves=20, reg_alpha=1.5, reg_lambda=3, feature_fraction=0.7, subsample=0.75, min_data_in_leaf=10, min_gain_to_split=0.01 |
| RF | metric=RMSE, ntree=800, nodesize=15, maxnodes=20 |
| SVM | metric=RMSE, method=svmRadial, trControl=ctrl, tuneLength=5 |

Table S3. Comparison of model performance across different encoding strategies

| Model | Data | R2 | RMSE | MAE |
| --- | --- | --- | --- | --- |
| LightGBM-missForest | Train | 0.904 | 10.97 | 7.19 |
|  | Test | 0.793 | 23.46 | 16.94 |
| LightGBM-N/A | Train | 0.875 | 12.47 | 8.36 |
|  | Test | 0.727 | 26.99 | 19.80 |
| LightGBM-average | Train | 0.883 | 12.09 | 8.16 |
|  | Test | 0.762 | 25.17 | 18.71 |
| LightGBM-median | Train | 0.885 | 11.99 | 8.12 |
|  | Test | 0.748 | 25.93 | 19.72 |
| RF-missForest | Train | 0.868 | 12.81 | 9.01 |
|  | Test | 0.816 | 22.15 | 17.99 |
| RF-average | Train | 0.855 | 13.45 | 9.63 |
|  | Test | 0.796 | 23.29 | 18.62 |
| RF-median | Train | 0.854 | 13.51 | 9.73 |
|  | Test | 0.777 | 24.39 | 19.48 |
| SVM-missForest | Train | 0.827 | 14.67 | 8.29 |
|  | Test | 0.714 | 17.61 | 20.30 |
| SVM-average | Train | 0.811 | 15.37 | 8.59 |
|  | Test | 0.709 | 27.87 | 20.33 |
| SVM-median | Train | 0.809 | 15.46 | 8.64 |
|  | Test | 0.673 | 29.53 | 21.16 |

Table S4. Physical properties of AgNPs and AuNPs synthesized for external validation and viability of HaCaT and HDFs cells upon treatment with different concentrations

| Sample | Reductant | Size （nm） | Zeta potential （mV） | Exposure concentration (mg/L) | HaCaT cell viability (%) | HDFs cell viability (%) |
| --- | --- | --- | --- | --- | --- | --- |
| AgNFs | Trisodium citrate Gallic acid | 105.00±20.74 | –32.24±0.43 | 6.25 | 99.16 | 92.15 |
|  |  |  |  | 12.5 | 97.97 | 89.88 |
|  |  |  |  | 25 | 96.64 | 83.23 |
|  |  |  |  | 50 | 82.30 | 78.91 |
| CHA- AgNPs | Chlorogenic acid | 10.07±3.13 | –35.90±0.53 | 12.5 | 92.2 | 85.19 |
|  |  |  |  | 25 | 86 | 79.95 |
|  |  |  |  | 50 | 77.4 | 72.31 |
|  |  |  |  | 100 | 65.8 | 69.89 |
| CTAB- AgNPs | CTAB | 27.51±3.99 | +15.60±1.41 | 6.25 | 82.39 | 83.39 |
|  |  |  |  | 12.5 | 75.87 | 81.27 |
|  |  |  |  | 25 | 62.25 | 77.31 |
|  |  |  |  | 50 | 56.93 | 70.79 |
| GA- AgNPs | Gallic acid | 17.71±3.96 | –16.90±0.43 | 6.25 | 99.33 | 92.06 |
|  |  |  |  | 12.5 | 97.23 | 91.17 |
|  |  |  |  | 25 | 93.58 | 86.07 |
|  |  |  |  | 50 | 80.46 | 84.94 |
| GA- AuNPs | Gallic acid | 29.00±2.93 | –36.77±0.65 | 6.25 | 98.51 | 92.17 |
|  |  |  |  | 12.5 | 94.06 | 87.76 |
|  |  |  |  | 25 | 88.19 | 84.28 |
|  |  |  |  | 50 | 83.33 | 79.91 |

Figure S1. Distribution of missing values in the database